ABSTRACT

A new titanium (IV) butoxide-cyanopropyltriethoxysilane (Ti-CNPrTEOS) hybrid material was successfully synthesized as sorbent for the extraction of polar aromatic amines. The sorbent was synthesized by hydrolysis and condensation of titanium (IV) butoxide and cyanopropyltriethoxysilane with the presence of hydrochloric acid as catalyst via sol-gel method. Under the optimum synthesis conditions (tetrahydrofuran as solvent, 1.2 M of hydrochloric acid catalyst, 4 mol of water content with ratio of titanium (IV) butoxide and cyanopropylteriethoxysilane of 1:1 and aging temperature of 60°C), the sorbents were characterized by Fourier Transform-Infrared, Field-Emission Scanning Electron Microscopy-Energy, CHN elemental analysis, Brunauer–Emmett–Teller (BET) desorption and thermogravimetric analysis. A solid phase extraction (SPE) method has been developed using Ti-CNPrTEOS sorbent for the determination of aromatic amines and optimum experimental conditions were sample at pH 7, dichloromethane as conditioning solvent, 10 mL sample loading volume, 5 mL of acetonitrile as the eluting solvent. The limit of detection (LOD) and limit of quantification (LOQ) using Ti-CNPrTEOS SPE sorbent (0.01-0.20; 0.03-0.61 µgL-1) were absolutely lower compared with those achieved using silica-cyanopropyl (Si-CN) SPE sorbent (0.23-1.47; 0.75-4.91 µgL-1) and C18 SPE sorbent (0.36-0.98; 1.54-2.56 µgL-1). The recoveries and repeatability obtained from water samples using the sol–gel Ti-CNPrTEOS SPE sorbent were 57–99% and RSDs 1–4%, n=5. The lowest recovery of non-polar diethylaniline, DEA (57%) indicated that the sorbent was very selective towards the extraction of polar aromatic amines. Ti-CNPrTEOS sorbent was also successfully applied as sorbent for solid phase membrane tip extraction (SPMTE). Under the optimum extraction conditions; 15 mL of sample at pH 7, acetonitrile as conditioning and desorption organic solvent, extraction time of 15 min and desorption time of 15 min, the method showed good linearity with acceptable reproducibility (RSD 2.5 – 3.6%, n = 5) and LOD and LOQ for Ti-CNPrTEOS SPMTE (0.13 – 6.23 ngL-1; 0.53 – 5.67 ngL-1) were lower with those achieved by C18-SPE (0.36-0.98 gL-1; 1.54-2.56 gL-1). The application of the Ti-CNPrTEOS SPMTE sorbent was successfully carried out by analysis of aromatic amines in river water sample with the recovery between 49–99%. The lowest recovery of non-polar DEA (49%) indicated that the sorbent was very selective towards the extraction of polar aromatic amines. The newly developed method using Ti-CNPrTEOS sorbent was proven as a simple, rapid, cheap and solvent efficient extraction technique.

ABSTRAK

Bahan baru titanium(IV) butoksida-cyanopropiltrietoksisilane (Ti-CNPrTEOS) telah berjaya disintesis sebagai penjerap untuk pengekstrakan aromatik amina kutub. Penjerap tersebut disintesis melalui hidrolisis dan kondensasi titanium(IV) butoksida dan cyanopropiltriethoksisilane dengan kehadiran asid hidroklorik sebagai pemangkin melalui metod sol-gel. Berdasarkan kepada kondisi sintesis optimum (tetrahidrofuran sebagai pelarut, 1.2 M kepekatan pemangkin asid hidroklorik, 4 mol kandungan air, nisbah 1:1 titanium(IV) butoksida dan cyanopropiltriethoksisilane dan suhu penuaan pada 60°C, penjerap tersebut dicirikan dengan menggunakan Fourier Transform-Inframerah, Field-Emission Scanning Electron Microscopy-Energy, analisis CHN elemen, penjerapan Brunauer–Emmett–Teller (BET) dan analisis termogravimetri. Kaedah pengekstrakan fasa pepejal (SPE) telah dibangunkan menggunakan penjerap Ti-CNPrTEOS dan kondisi eksperimen optimum adalah sampel pada pH 7, diklorometana sebagai pelarut melembap, 10 mL isipadu muatan sampel, 5 mL acetonitril sebagai pelarut pengeluar. Had pengesan, LOD dan had kuantiti, LOQ untuk penjerap Ti-CNPrTEOS-SPE (0.01–0.20; 0.03-0.61µgL-1) menunjukan keputusan yang lebih rendah berbanding yang diperolehi menggunakan penjerap Si-CN SPE (0.23-1.47; 0.75-4.91 µgL-1) dan penjerap C18-SPE (0.36-0.98; 1.54-2.56 µgL-1) dengan selektiviti lebih tinggi untuk pengekstrakan aromatik amina kutub. Kebolehulangan yang diperolehi daripada sampel air menggunakan penjerap Ti-CNPrTEOS SPE adalah 57-99% dan RSD 1-4%. Kebolehulangan terendah untuk dietilanilin, DEA tidak kutub (57%) menunjukkan penjerap adalah lebih selektif terhadap pengekstrakan aromatik amina kutub. Penjerap Ti-CNPrTEOS telah berjaya digunakan sebagai penjerap untuk pengekstrakan membran tip fasa pepejal (SPMTE). Berdasarkan kondisi pengekstrakan optimum; 15 mL sampel pada pH 7, acetonitril sebagai pelarut organik pelembap dan penyahjerap, masa pengekstrakan 15 min dan masa penyahjerap 15 min, kaedah ini menunjukkan julat linear yang baik dengan kebolehulangan yang diterima pakai (RSD 2.5–3.6%, n = 5), LOD dan LOQ (0.13 – 6.23 ngL-1; 0.53–5.67 ngL-1) adalah lebih rendah berbanding yang dicapai melalui C18-SPE (0.36-0.98 gL-1; 1.54-2.56 gL-1). Kebolehulangan yang diperolehi daripada sampel air menggunakan penjerap Ti-CNPrTEOS SPMTE adalah 49-99% dan RSD 1-4%. Kebolehulangan terendah untuk DEA yang tidak kutub (49%) menunjukkan penjerap adalah lebih selektif terhadap pengekstrakan aromatik amina kutub.Ti-CNPrTEOS telah terbukti teknik pengekstrakan yang mudah dan efektif masa, kos dan pelarut.

ACKNOWLEDGEMENTS

Syukur Alhamdulillah, all praises to Allah, the supreme Lord of the universe.

First of all, I would like to express my deepest gratitude to my supervisors, Associate Professor Dr. Nor Kartini Abu Bakar and Dr. Sharifah Mohamad, for their constant ideas and enthusiasm. Their excellent scientific guidance, infinite patience and unconditional helps have enabled me to approach work positively. Thanks to the laboratory assistants of the Department of Chemistry, Faculty of Science, University of Malaya, particulary to Pn. Ruhaida Bahru for the technical assistance.

I would like to express my thanks to all post-graduate friends and staffs in Analytical Chemistry Postgraduate Research Laboratory. I would like to take this opportunity to thank everyone who has contributed either directly or indirectly to this project.

I would also like to thank the University of Malaya for the facilitations and financial support (Grant: PV 096-2011A) and International Islamic University Malaysia, the Ministry of Higher Education (MOHE) Malaysia for fellowship for myself.

To my beloved husband and families, I cannot thank them enough for their support and faith in me.

TABLE OF CONTENTS

CHAPTER				TITLE				PAGE

ABSTRACT							     iii

ABSTRAK							     iv

ACKNOWLEDGEMENTS					     v

TABLE OF CONTENTS					     vi

LIST OF FIGURES						     x

LIST OF TABLES						     xv

LIST OF ABBREVIATIONS				     xvii

LIST OF SYMBOLS					     xix

1		INTRODUCTION

1.1	Introduction						     1

1.2	Statement of Problems				     3

1.3	Objectives of the Research		                             7

1.4	Scope of Study					     8

1.5	Outline of the Thesis					     8

2		LITERATURE REVIEW

  - Sol-Gel Technology					    10

  - Starting Materials					    13

    - Titania Alkoxide			   	    13

2.2.2    3-cyanopropyltriethoxysilane		                16

2.3	Sol-gel Preparation			     		   18

2.4	Extraction Methods for Chemical Analysis		    24

2.4.1	Liquid-Liquid Extraction (LLE)		    25

2.4.2	Solid Phase Extraction (SPE)			    26

2.4.3	Solid Phase Microextraction (SPME)		    29

2.4.4	Stir Bar Sorptive Extraction (SBSE)		    29

2.4.5	Solid Phase Membrane Tip Extraction 	     31

(SPMTE)

2.4.6	Extraction Using Sol-gel Sorbents		     33

2.5	Aromatic Amines					     39

2.5.1	Extraction of Aromatic Amines		     40

3		RESEARCH METHODOLOGY							3.1	Chemicals, Materials and Reagents			     45

3.2	Instruments						     49

3.3	Preparation of Ti-CNPrTEOS Sorbent		     49

3.4	Gas Chromatography-Flame Ionization Detector           50

Analysis

3.5	Solid Phase Extraction Procedure			     50

3.5.1	Optimization of Extraction Parameters and	     52

Practical Considerations

3.6	Solid Phase Membrane Tip Extraction Procedures	     54

3.6.1	Optimization of Extraction Parameters and 	    56

Practical Considerations

3.7 	Analysis of Water Samples				     57

3.7.1	Sampling and Pretreatment of Samples	     57

3.7.2	Spiking				  	     58

3.8	Method Validation				                 58

3.8.1	Limit of Detection	     	                 	     59

3.8.2	Recovery					     60

3.8.3	Precision					     60

4	PREPARtion and characterization of new

sol-gel titanium (I V) Butoxide-CYanopropyltriethoxysilane hybrid

sorbent for the extraction of polar

Aromatic amines

  - Mechanism of the Reactions				     62

  - FTIR Analysis						     64

# Thermogravimetric Analysis			 	     66

# Surface Morphology of Ti-CNPrTEOS Sorbent 	     68

  - Optimization of Ti-CNPrTEOS Sorbent Synthesis         71

Parameters

4.5.1 	Selection of Solvents				     71

4.5.2	Concentration of Acid Catalyst		     71					4.5.3	Water Content              			     73

4.5.4	Ratio Study					     75

4.5.5	Aging Temperature				     77

  - Conclusions						     79

5 		Optimization of solid phase extraction

for the determination of polar aromatic

amines using new sol-gel titanium (IV)

butoxide-cyanopropyltriethoxysilane sorbent

5.1	Optimization of Solid Phase Extraction Parameters	     81

    - Sample pH			                    	     81

    - Conditioning Solvents			        	     83

    - Sample Loading Volumes		        	     84

    - Washing Solvents		                    	     86

    - Elution Solvents		                   	     88

    - Volume of Elution Solvents	                 	     89

  - Method Validation				                 90

  - Real Sample Analysis					     93

  - Conclusions						     96

6 	THE APPLICATION OF SOL-GEL SYNTHESIZED titanium (IV) butoxide-cyanopropyltriethoxysilane AS solid phase membrane tip extraction protected sorbent

6.1	Optimization of Solid Phase Membrane Tip

Extraction Parameters					    97

6.1.1	Sample pH					    97

6.1.2	Conditioning Solvent			    	    99

6.1.3	Sample Volume				    100

6.1.4	Extraction Time				    101

6.1.5	Desorption Solvents				    104

6.1.6	Desorption Time				    105

6.2	Method Validation					    107

6.3	Real Sample Analysis					    108

6.4	Conclusions						    113

## 7		CONCLUSIONS AND FUTURE DIRECTIONS

## 7.1	Conclusions						    114

## 7.2	Future Directions					    117

## REFERENCES								    119

## APPENDIX									    131

LIST OF FIGURES

| FIGURE NO. | TITLE | PAGE |
| --- | --- | --- |
| 2.1 | Formation of various products via sol-gel technology. | 11 |
| 2.2 | Molecular structure of titanium (IV) butoxide | 15 |
| 2.3 | Molecular structure of 3-cyanopropyltriethoxysilane | 17 |
| 2.4 | Schematics of (a) the SPMTE setup and (b) expanded view of dynamic SPMTE | 32 |
| 2.5 | Number of publications on extractions using sol-gel sorbents according to year | 33 |
| 3.1 | Schematic diagram of SPE procedure | 51 |
| 3.2 | Schematic diagram of SPMTE setup. | 55 |
| 4.1 | (a) Catalytic hydrolysis of Ti(OBu)4, (b) Catalytic hydrolysis of 3-CNPrTEOS, (c) Growth of sol-gel Ti-CNPrTEOS chain via polycondensation reaction of hydrolyzed Ti(OBu)4 and CNPrTEOS | 63 |
| 4.2 | FTIR spectrum; (a) Pure CNPrTEOS, (b) Pure Ti(OBu)4, (c) sol gel Ti-CNPrTEOS | 65 |
| 4.3 | TGA profiles; (a) Pure CNPrTEOS, (b) sol gel Ti-CNPrTEOS | 66 |
| 4.4 | FESEM images; (a) magnification of 5.00K, (b) magnification of 15.00K | 68 |
| 4.5 | N2 adsorption-desorption isotherm of Ti-CNPrTEOS and blank Ti | 70 |
| 4.6 | Effect of acid catalyst of 1:1 molar ratio Ti(OBu)4:CNPrTEOS on the extraction efficiency of aromatic amines. Extraction conditions: 10 mg of Ti-CNPrTEOS sorbent, 10 mL of 10 mg L−1 aromatic amines mixture and 15 min extraction time. Sol–gel synthesis condition: THF as solvent, 4 moles of water content, 1:1 molar ratio Ti(OBu)4:CNPrTEOS and aging temperature of 50°C for 24h. | 72 |
| 4.7 | Effect of water content of 1:1 molar ratio Ti(OBu)4:CNPrTEOS on the recovery of aromatic amines. Extraction conditions: 10 mg of Ti-CNPrTEOS sorbent, 10 mL of 10 ppm aromatic amines mixture and 15 min extraction time. Sol–gel synthesis condition: THF as solvent, 3 M of HCl catalyst, 1:1 molar ratio Ti(OBu)4:CNPrTEOS and aging temperature of 50°C for 24h. | 74 |
| 4.8 | Effect of molar ratio Ti(OBu)4:CNPrTEOS on the recovery of aromatic amines. Extraction conditions: 10 mg of Ti-CNPrTEOS sorbent, 10 mL of 10 ppm aromatic amines mixture and 15 min extraction time. Sol–gel synthesis condition: THF as solvent, 3 M of HCl catalyst, 4 moles of water content and aging temperature of 50°C for 24h. | 77 |
| 4.9 | Effect of aging temperature on the recovery of aromatic amines. Extraction conditions: 10 mg of Ti-CNPrTEOS sorbent, 10 mL of 10 ppm aromatic amines mixture and 15 min extraction time. Sol–gel synthesis condition: THF as solvent, 3 M of HCl catalyst, 1:1 molar ratio Ti(OBu)4:CNPrTEOS and 4 moles of water content. | 78 |
| 5.1 | Effect of pH of analytes mixture on the recovery of aromatic amines. Extraction conditions: toluene as conditioning solvent, 5 mL sample loading volume, acetonitrile as the eluting solvent and 10 mL of elution solvent | 83 |
| 5.2 | Effect of conditioning solvent on the recovery of aromatic amines. Extraction conditions: sample at pH 7, 5 mL sample loading volume, dichloromethane as washing solvent, acetonitrile as the eluting solvent and 10 mL of elution solvent | 84 |
| 5.3 | Effect of sample loading volume on the recovery of aromatic amines. Extraction conditions: sample at pH 7, dichloromethane as conditioning solvent, dichloromethane as washing solvent, acetonitrile as the eluting solvent and 10 mL of elution solvent. | 85 |
| 5.4 | Effect of washing solvent on the recovery of aromatic amines. Extraction conditions: sample at pH 7, dichloromethane as conditioning solvent, 10 mL sample loading volume and 10 mL of elution solvent. | 87 |
| 5.5 | Effect of eluting solvent on the recovery of aromatic amines. Extraction conditions: sample at pH 7, dichloromethane as conditioning solvent, drying for 30 min, 10 mL sample loading volume and 10 mL of elution solvent. | 88 |
| 5.6 | Effect of eluting solvent volume on the recovery of aromatic amines. Extraction conditions: sample at pH 7, dichloromethane as conditioning solvent, drying for 30 min, 10 mL sample loading volume, acetonitrile as the eluting solvent. | 90 |
| 5.7 | Chromatograms of Ti-CNPrTEOS SPE; (a) blank waste water, (b) spiked waste water (c) blank river water, (d) spiked river water, (e) blank tap water, (f) spiked tap water. Peaks: 1. Aniline; 2. m-toluidine; 3. N,N-dimethylaniline; 4. N,N-diethylaniline; 5. 4-ethylaniline; 6. Ethylaniline. | 94 |
| 6.1 | Effect of pH on SPMTE. Extraction conditions: 1µg L-1 of spiked solution; sample volume: 10 mL; organic solvent : methanol; extraction time: 10 min; desorption time: 15 min; desorption solvent: 200 µL of acetonitrile; no adjustment of sample pH and salt. | 98 |
| 6.2 | Effect of sample volume on SPMTE. Extraction conditions: 1µg L-1 of spiked solution; sample pH 7; organic solvent: methanol; extraction time: 10 min; desorption time: 15 min; desorption solvent: 200 µL of acetonitrile. | 100 |
| 6.3 | Effect of organic solvent on SPMTE. Extraction conditions: 1µg L-1 of spiked solution; 15 mL of sample at pH 7; extraction time: 10 min; desorption time: 15 min; desorption solvent: 200 µL of acetonitrile | 102 |
| 6.4 | Effect of extraction time on SPMTE. Extraction conditions: 1µg L-1 of spiked solution; sample pH 7; sample volume: 15 mL; organic solvent: methanol; desorption time: 15 min; desorption solvent: 200 µL of acetonitrile | 103 |
| 6.5 | Effect of desorption solvent on SPMTE. Extraction conditions: 1µg L-1 of spiked solution; sample pH 7; sample volume: 15 mL; organic solvent: methanol; extraction time : 15 min; desorption time: 15 min; desorption solvent: 200 µL | 105 |
| 6.6 | Effect of desorption time on SPMTE. Extraction conditions: 1µg L-1 of spiked solution; sample pH 7; sample volume: 15 mL; organic solvent: methanol; extraction time : 15 min; desorption solvent: 200 µL of acetonitrile. | 106 |
| 6.7 | Chromatograms of river water analysis; (a) unspiked river water using Ti-CNPrTEOS SPE, (b) spiked unspiked river water using Ti-CNPrTEOS SPE, (c) unspiked river water using C18 SPE, (b) spiked unspiked river water using C18 SPE Peaks: 1. Aniline; 2. m-toluidine; 3. N,N-dimethylaniline; 4. N,N-diethylaniline; 5. 4-ethylaniline; 6. Ethylaniline. . | 112 |

## LIST OF TABLES

| TABLE NO. | TITLE | PAGE |
| --- | --- | --- |
| 2.1 | Sol-gel preparations | 22 |
| 2.2 | Properties of commercially available solid phase extraction sorbents | 28 |
| 2.3 | Commercially available SPME fibers | 30 |
| 2.4 | Summary of sol-gel sorbents in SPE, SPME and SBSE | 34 |
| 2.5 | Summary of the extraction of aromatic amines | 41 |
| 3.1 | Structure and properties of aromatic amines | 46 |
| 3.2 | Name, function and chemical structure of the sol-gel ingredients for Ti-CNPrTEOS sorbent | 48 |
| 4.1 | BET pore size and surface area | 69 |
| 4.2 | CHN elemental analysis of Ti-CNPrTEOS | 76 |
| 5.1 | Qualitative data comparisons between sol–gel Ti-CNPrTEOS SPE, Si-CN SPE and C18 SPE: linearity, repeatability (% RSD, n = 5), limit of detection and limit of quantification of aromatic amines | 92 |
| 5.2 | Percentage recovery and % RSD (n = 3) for spiked aromatic amines from river water samples using developed sol–gel Ti-CNPrTEOS SPE, Si-CN SPE and C18 SPE method with GC–FID analysis. | 95 |
| 6.1 | Qualitative data comparisons between sol–gel Ti-CNPrTEOS SPMTE and C18 SPE; linearity, repeatability (% RSD, n = 5), limit of detection and limit of quantification of aromatic amines | 110 |
| 6.2 | Percentage recovery and % RSD (n = 3) for spiked aromatic amines from river water samples using developed sol–gel Ti-CNPrTEOS SPMTE, and C18 SPE method with GC–FID analysis. | 111 |

LIST OF ABBREVIATIONS

CE		-	Capillary electrophoresis

CGE		-	Capillary gel electrophoresis

CIEF		-	Capillary isoelectric focusing

CITP		-	Capillary isotachophoresis

CSM		-	Cone-shaped membrane

CTAB		-	Cetyltrimethylammonium bromide

CZE		-	Capillary zone electrophoresis

DAD		 -	Diode-Array Detector

DC		-	Direct current

ESI-MS	-	Electrospray ionization mass spectrometry

EU		-	European Union

FESI		-	Field enhanced sample injection

GC		-	Gas chromatography

GLUF		-	Glufosinate

GLYP		-	Glyphosate

HCl		-	Hydrochloric acid

HF		-	Hollow fiber

HF-LPME	-	Hollow fiber liquid phase microextraction

His		-	Histidine

HPLC		-	High Performance Liquid Chromatography

IDA		-	Iminodiacetic acid

IP		-	Ion-pair

IS		-	Internal standard

IUPAC	-	International Union of Pure and Applied Chemistry

LC		-	Liquid chromatography

LIF		-	Laser-induced fluorescence

LLE		-	Liquid-liquid extraction

LOD		 -	Limit of Detection

LOQ		-	 Limit of Quantification

LPME		-	Liquid phase microextraction

LPMTE	-	Liquid phase membrane tip extraction

LODs		-	Limits of detection

LVSS		-	Large volume sample stacking

MAE		-	Microwave assisted extraction

MeOH		-	Methanol

MES		-	2-(N-morpholino)ethanesulfonic acid

MIP		-	Molecular imprinted polymer

MRL		-	Maximum residue limit

MWCNTs	-	Multiwall carbon nanotubes

NIM		-	Normal injection mode

PAHs		-	Polycyclic aromatic hydrocarbons

PDMS		-	Polydimethylsiloxane

PGC		-	Porous graphitic carbon

PP		-	Polypropylene

PS-DVB	-	Poly(styrene-divinylbenzene)

RP-HPLC	-	Reversed-phase High Performance Liquid Chromatography

RSD		-	Relative standard deviation

SBSE		-	Stir bar sorptive extraction

SFE		-	Supercritical fluid extraction

SPE		-	Solid phase extraction

SPME		-	Solid phase microextraction

SPMTE	-	Solid phase membrane tip extraction

USEPA	-	United States Environmental Protection Agency

UV		-	Ultra violet

EU		-	 European Union

LIST OF symbols

i		-	Analyte

K		-	Partition coefficient

C		-	Analyte concentration

R		-	Extraction recovery

E		-	Enrichment

V		-	Volume

-	Mobile phase viscosity

T		-	Absolute Temperature

∆P 		-	Pressure drop

-	Flow resistant factor

L		-	Column length

u		-	Linear flow rate

dP		-	Particle diameter

H		-	Theoretical plate height

I.D.		-	Internal diameter

nA 		-	Amount (mass) of analyte extracted

F		-	Detector response factor

m		-	Mass of analyte

ɛ°		-	Elution strength